## Slide 1: The giant plasticity of a quantum crystal
S. Balibar, A. Fefferman, A. Haziot, X. Rojas
Laboratoire de Physique Statistique,
Ecole Normale Supérieure and CNRS,
associated to the Universities Paris 6 & 7, Paris (France),
and J. Beamish (Edmonton, Canada)
other collaborations: M.H.W. Chan and J. West (Penn State) ,
H.J. Maris (Brown University)
Workshop nanostructures,
P.M. Curie University , Nov. 30th , 2012

## Slide 2: ultrapure 4He single crystals do not resist to shear around 0.2K
dislocations are highly mobile in a T-domain between
- 3He impurity pinning at low T
- damping from collisions with thermal phonons at higher T
a hexagonal 4He crystal.
a direct measurement of its shear modulus
Haziot et al. submitted to Phys. Rev. Lett. (2012)
a giant plasticity with no equivalent in classical crystals
We have solved the « enigma of supersolidity ».
strong softening around 0.2K

## Slide 3: plasticity of a crystal: dislocation gliding
under larger stress s
the strain e is the sum of
elat due to the deformation of the lattice and
edis due to the displacement of dislocations
= meff (elat + edis)
an effective shear modulus meff
If dislocations move,
meff is reduced
a shear stress
under small stresses: elastic deformation of the lattice determined by elastic coefficients

## Slide 4: original motivation: the enigma of supersolidity
E. Kim and M. Chan (Penn. State U. 2004):
a « torsional oscillator » (~1 kHz)
a change in the resonance period below ~100 mK
a small critical velocity
1 % of the solid mass decouples : Leggett’s « NCRI »?
rigid axis
( Be-Cu)
solid He
in a box
excitation
detection
the resonance period
depends on the inertia momentum I and on the torsion constant K
supersolidity appears (I decreases) ?
or a change in stiffness (K increases) ?
temperature (K)
period (ms)

## Slide 5: Direct shear modulus measurements: the method invented by Day and Beamish (2007):
piezoelectric shear transducers
solid 4He
I
an ac- voltage V
produces a deformation e
and a shear stress s
on the other transducer
inducing a current
I=w d152 mV/d
gap d ~1 mm
at ENS in 2012 we calibrated the measurement of m=s/e on single crystals

## Slide 6
a model for the elastic anomaly:
pinning of dislocations by impurities (Beamish et al. 2008)
Syshchenko Day and Beamish (PRL 2010) : a distribution for EB 0.73 ± 0.45 K
calculation by Corboz et al. 2008 : 0.8 ± 0.1 K
at high T
at low T
network pinning
impurity pinning
 crossover 
dislocations are pinned by 3He impurities below a temperature which depends on
the binding energy EB,
the 3He concentration X3
the dislocation density L
mobile dislocations => soft cystal
pinned dislocations => stiff crystal
large plasticity if dislocations move easily
Compare high quality single crystals grown at ENS
with Beamish’s polycrystals

## Slide 7
ENS Paris 2012:
direct measurements on oriented single crystals from 0.015 to 1K
orientation from growth shape of a seed
growth inside the 1.2 mm gap between 2 transducers
very small vertical displacement ~ 0.001 Angström
strain e down to 10-10
0.2 Hz to 20 kHz
vertical stress component s down to 10-9 bar

## Slide 8
the « loading curve » in our cell #2
the measured shear modulus increases linearly
with the level of the solid
in the 0.7 mm gap
between the 2 transducers
0.7 mm gap

## Slide 9
random nucleation on various sites:
many crystals with different orientations
X2
X15
X6
X3
X5
X21
X20

## Slide 10
Orientation : θ=89.5° ; φ=75°
measured shear modulus:
σ = 0.0001(c11-2c13+c33) + 0.933c44 + 0.067c66
depends mainly on c44
orientation X2
c
θ
φ
x
z
y
c

## Slide 11: the elasticity tensor of hcp crystals
simple shear involve only c44 or c66:
the transverse sound velocity along c involves xz or yz shear and is given by
the transverse sound velocity inside the basal plane involves xy shear and is given by
6 elastic coefficients cij
If z is parallel to the 6-fold symmetry axis c or [0001], the indices i,j from 1 to 6 mean respectively xx, yy, zz, yz, xz, and xy with
c66 = (c11 – c12)/2

## Slide 12
Orientation : θ=89.5° ; φ=75°
measured shear modulus:
σ = 0.0001(c11-2c13+c33) + 0.933c44 + 0.067c66
depends mainly on c44
prediction from measurements by Crepeau at 1.32K and by Greywall at 1.2K where dislocations cannot move at 10 MHz:
σstiff= 122 bar
orientation X2
c
θ
φ
x
z
y
c

## Slide 13
Orientation : θ=45° ; φ=85°
measured shear modulus: σ=0.248 (c11-2.c13+c33) + 0.0038c44 + 0.0038c66
negligible dependence on c44 and c66
predicted stiff state: mstiff = 187 bar
orientation X3

## Slide 14
orientation X5
orientation : θ=60° ; φ=30°
measured shear modulus : σ=0.047 (c33 + c12 – 2 c13 ) + 0.25 c44 + 0.56 c66
large dependence on c66
predicted stiff state: mstiff = 1.19 107 Pa = 119 bar
c

## Slide 15
a polycrystal grown at constant V (“blocked capillary method”)
final growth pressure : 33.8 bar
predicted stiff state using HJ Maris’ averaging method: mstiff = 144 bar
melting shows grain boundaries. Small grains
ripening from the top in a few minutes

## Slide 16
X3 is tilted by ~ 45°
no dependence on c44 nor c66
no T-variation m = 187 bar
=> c11, c13 and c33 are constant
=> calibration of transducers 0.88 A/V in cell #1, 0.95 A/V in cell#2
the softening is highly anisotropic
(A. Haziot et al. submitted to Phys Rev Lett. October 2012)
X3
X2 depends ~ only on c44
X5 depends more on c66 than c44
X2
X5
at low T for all crystals, agreement with measurements at 10MHz and high T by Crepeau (1.32K) and Greywall (1.2K),
the « supersolid » is not stiffer than the normal solid contrary to Anderson’s prediction.
polycrystal BC1:
intermediate T-variation
BC1

## Slide 17
What is the origin of the large anisotropy of the plasticity ?
single crystal X3 c at 45° :
no dependence on c44 nor c66
no T-variation => calibration
X3
X2 and X21 depend ~ only on c44
X5 depends more on c66 than c44
X2
X5
The magnitude of the change in shear modulus depends on orientation
Dislocations glide along dense planes.
Basal planes ? the variation of m should be due to c44
Prismatic planes ? it should be c66
polycrystal BC1:
intermediate T-variation
BC1

## Slide 18
dislocations glide only parallel to the basal planes
X2, X5, X6 and X21 :
all grown at 1.4K, natural purity should have the same elastic constants
If dislocations glide along the basal planes,
c66 = Cst and c44 varies :
62±8% reduction in c44 for all crystals
an expected results for hcp crystals ? may be,
but hexagonal metals show gliding either along basal planes (0001): Be, Mg, Co, Zn
or along the prismatic planes (10-10) perp to the basal planes : Zr, Ti
Assuming the opposite (c44 contant, c66 varies ) leads to absurd results
X5 varies less than X2 with a stronger dependence on c66! c66 should vary by 300% for X6 and by > 1000% for X21 !
X21

## Slide 19: amplitude dependence at 20 mK - hysteresis
crystals grown at 1.4K,
no liquid in the cell
X6, X2 and X5:
the threshold stress
s = 1 microbar
corresponds to the stress necessary for dislocations to break away from 3He impurities
hysteresis because the force depends on the distance between bound impurities
X4 cooled down at high drive
with liquid in the cell
X4 cooled down at high drive
with liquid in the cell
« resolved » = projected in the basal plane

## Slide 20: with no impurities at all, dislocations move freely
crystals grown at 1.4K,
no liquid in the cell
X4 cooled under large strain
in the presence of liquid He
all 3He expelled into the liquid
stable soft state even when reducing the strain down to 10-10
80% reduction in c44
a very large softening with no equivalent in classical crystals
X4 cooled down at high drive
with liquid in the cell
X4 cooled down at high drive
with liquid in the cell
« resolved » = projected in the basal plane

## Slide 21
« zone melting » with 4He : from 0.3 ppm 3He to 0.4 ppb
… and down to zero
Slow growth proceeds very close to equilibrium at the solid-liquid interface.
The concentration ratio is
at 25 mK:
starting with X3L = 4 10-10
one obtains X3h = 4 10-31 !
even in the presence of dislocations, no 3He in the crystals grown below 25 mK
shaking the dislocations in the presence of some liquid expels all 3He in the liquid
=> the crystal is stable in a soft state
(C.Pantalei , X. Rojas and S. Balibar, JLTP 2010
using
D.O. Edwards and S.Balibar Phys. Rev. B 1989

## Slide 22: wT3 dissipation for collisions with thermal phonons
we measure the dissipation from the phase shift of the response
the 3He binding and the reduction in c44 depend on amplitude and purity
Granato and Lücke 1956 + Ninomiya 1974 predict a shear modulus variation
and a dissipation for phonon damping
If true, the dislocation density L
and the free length L between pinning sites
can be determined independently
high purity
low purity
low drive
high
drive
high
purity
low
purity

## Slide 23: a measurement of dislocation density and pinning length for various crystals (Haziot et al. to be published)
densities from 3 104 to 6 105 cm-2
pinning lengths from 60 to 230 mm
LL2 from 17 to 57
instead of 3 for a simple 3D lattice
=> dislocations are grouped in sub-boundaries
The best crystals are grown at low T.
the Shevchenko theory of a network of
superfluid dislocation cores
would require 1012 disloc/cm2 for a 1% NCRI
excellent agreement with 1/Q ~ wT3
collisions with thermal phonons
(very large damping at 10MHz and 1.2K
in Greywall’s experiment)

## Slide 24
dislocation motion:
comparison with a classical crystal
In Helium :
80% reduction in c44 => the plastic strain ed is 4 times larger than
the elastic strain el even for stresses 10-11 times the shear modulus
dislocations move like little violin strings
~ 1 mm at 10 kHz under stresses s ~ 0.6 mbar
typical velocities up to 6 cm/s
the plasticity exists at very low T,
it is giant at very low stress, reversible, linear,
fast, and anisotropic
In Copper (Tinder and Washburn (1964) plasticity is very much smaller even at room T:
160 times smaller under stresses 105 times larger (10-6 times the shear modulus)
irreversible and slow (minutes)
Ln
δl
dl ~ L b/ed with b = 3.6 Angstrom and
the dislocation density L ~ 104 cm-2
An interesting question:
do dislocations move by quantum tunneling through non-zero « Peierls » barriers or
classically with zero barriers ?

## Slide 25
back to supersolidity:
a possible artifact in « torsional oscillator » experiments:
J. Beamish, A. Fefferman, A. Haziot, X. Rojas, and S. Balibar, Phys Rev B 2012
when the « torsion rod » is a torsion tube:
r0 : outer radius of the tube
r1: inner radius
solid line: maximum possible effect of the He stiffness
In at least 4 cases the observed frequency could be a consequence of a 20 to 40% change in the He stiffness
the magnitude of the dissipation peak also agrees with the mechanical dissipation in stiffness measurements
the « critical velocity » would be the critical strain for unpinning of 3He (2 to 6 10-8 as measured by Day 2007 and by Rojas 2010)
more possible artifacts have been found in 2012 by Maris, Reppy, Chan … but some experiments (Kim, Kono, Shirahama…) resist to possible critics

## Slide 26: Conclusion: giant plasticity or supersolidity or both ?
the existence of superplasticity is now well established.
Solid 4He is « a probe in Materials Science » (P. Nozières 1994)
to be studied:
the distribution of pinning lengths from the stress dependence
the distribution of pinning energies from the frequency dependence
quantum tunneling or negligible kink energy ?
larger strains and more defects
the limit of zero dislocation and zero impurity
the existence of supersolidity would need stronger evidence…
and support from a convincing theory